## Slide 1: M504 - Asbestos types and properties

## Slide 2: Asbestos – what is it?
Naturally occurring fibrous silicate minerals
  Wide range of useful properties have led to it being used in many products since ancient times
  Was commercially mined in many countries
    Canada, South Africa, Russia, Zimbabwe, China, USA, Italy, Australia, Cyprus etc
  Chrysotile is the most common asbestos mineral
    (about 90% of asbestos mined)

## Slide 3: Asbestos – people at risk?
Evidence of harmful effects from asbestos exposure became apparent during the 20th century
Workers initially found to be at risk
  Asbestos miners
  Asbestos insulation installers (laggers)
  Asbestos textile workers
  (Groups with very high exposure levels)
Occurrence of asbestosis documented first, followed later by increased risk of lung cancer and then mesothelioma
As use of asbestos insulating board increased – builders and construction trades exposed to high levels of asbestos

## Slide 4: Asbestos – people at risk?
Production and use of asbestos products in UK, USA etc declined from mid 1970’s and the very high exposure levels previously encountered have largely ceased
In these countries, workers most at risk now are those that may inadvertently disturb asbestos products during repair and refurbishment work
However, in some countries asbestos is still being used, or use only recently stopped. In these countries, the potential for high exposure levels is much greater
In all cases a comprehensive asbestos management system should be in place

## Slide 5: Asbestos – 6 different minerals
Serpentine group
  Chrysotile - white asbestos
Amphibole group
  Amosite - brown asbestos (grunerite)
  Crocidolite - blue asbestos (riebeckite)
    Anthophyllite
    Tremolite
    Actinolite

## Slide 6
Chrysotile, amosite and crocidolite fibres

## Slide 7: Asbestos fibre properties
Occur as bundles of fibres
  Easily separated
  Can split into thinner fibres
High tensile strength
High length / diameter (aspect) ratios
  Minimum of 20 – can be up to 1000
Sufficiently flexible to be spun

## Slide 8: Structure of asbestos fibres
Amphibole
  Crystalline structure – chain silicate
  Different amphiboles distinguished by variations in chemical composition
  Fibres are generally straighter, more brittle and split into finer fibres more readily than serpentine
Serpentine
  Crystalline structure – sheet silicate
  ‘Scroll-like’ structure
  Fibres are less straight, more flexible and less liable to split into finer fibres compared to the amphiboles

## Slide 11: Properties of asbestos fibres
Industrial applications of asbestos take advantage of a combination of properties
  Use of fibre as reinforcing material largely dependent on length of fibre
  Other properties that make asbestos useful include
    Flexibility
    High tensile strength
    Non-combustibility
    Resistance to heat
    Low electrical conductivity
    Resistance to chemical attack

## Slide 12: Properties of asbestos fibres
Flexibility
  Chrysotile much more flexible than the amphiboles
  It is more suitable for weaving into a material and has been preferentially used in textiles and paper products
Tensile strength
  Similar for crocidolite, amosite, chrysotile
Effect of high temperatures on tensile strength
  Chrysotile – largely unaffected up to 550oC. Above this temperature dehydroxylation occurs with resulting rapid loss of tensile strength
  Amphiboles – tensile strength decreases after exposure to temperatures above 200oC, with dehydroxylation occurring above 400oC

## Slide 13: Properties of asbestos fibres
Combustibility
  Asbestos fibres do not burn, although will undergo changes at high temperatures
    Widespread use as fire-proofing
Thermal conductivity
  All asbestos types have very low thermal conductivities – i.e. they are all very good insulating materials
    Widespread use in thermal insulation and lagging

## Slide 14: Properties of asbestos fibres
Resistance to chemical attack
  Generally unaffected by water
  Exposure to acids can lead to some breakdown of the asbestos fibres
  Chrysotile has very low resistance to acid attack
  Amphiboles (particularly crocidolite) much more resistant to acid attack
    Crocidolite widely used where resistance to chemical (acid) attack is required e.g. gaskets in chemical plant and gas production plant

## Slide 15: Properties of asbestos fibres
Resistance to chemical attack
  For exposure to alkalis chrysotile is the most resistant to attack, with amphiboles being slightly less resistant
    Chrysotile widely used in cement products
    Chrysotile is hydrophilic (easily wetted)
    Amphibole asbestos are more hydrophobic (not easily wetted)

## Slide 16: Properties of asbestos fibres
Effects of thermal degradation
  Main effect of high temperature is to cause dehydroxylation (loss of water of crystallisation from the mineral)
    Chrysotile – dehydroxylation occurs between 550 – 750 oC
    Amphiboles – dehydroxylation occurs between 400 – 600 oC
  Thermal decomposition can cause oxidation of iron in the mineral leading to colour changes
    Amosite – pale brown to dark brown
    Crocidolite – blue to dark blue / black

## Slide 17: Uses of asbestos
Widespread uses of asbestos include
  Thermal and acoustic insulation
  Spray coating (as fire protection)
  Asbestos reinforced building board
  Asbestos reinforced cement products
  Plastic products (e.g. vinyl floor tiles)
  Textiles
  Friction materials (brake pads etc)
  Gaskets and packing materials
  Roofing felts etc
Any type of asbestos may have been used, however, for some products some types of asbestos are more likely

## Slide 28: Asbestos - contaminants
Asbestos is sometimes found as a contaminant in other minerals being mined or extracted e.g. iron ore, vermiculite and talc
  Historically substances such as industrial talc may have been contaminated with asbestos (particularly tremolite)
Some deposits of chrysotile have been found to be contain small quantities of amphibole minerals such as tremolite

## Slide 29: Man made mineral fibres (MMMF)
Large group of synthetic materials manufactured from molten glass, rock, slag or clays
  Glass wool or glass fibre, rock wool and slag wool
    Widely used for thermal and acoustic insulation, fire protection and as reinforcing material in building products such as ceiling tiles
  Continuous filament fibres
    Long fibres woven into cloth or used in manufacture of electrical insulators and to reinforce plastics and other materials
  Refractory ceramic fibres
    Used in building boards and where high temperature insulation properties are required (e.g. in furnaces)
    Based on pure alumina or zirconia or mixtures of alumina and silica

## Slide 30: Machine made mineral fibres
Machine made mineral fibres typically have fibre diameters much larger than asbestos fibres
  Glass wool, rock wool, slag wool diameters of 1 to 10 micron but typically within the range 4 – 9 micron
  Continuous filament fibre diameters of 6 – 15 micron but typically within the range 8 – 10 micron
  Refractory ceramic fibres have diameters around 1 – 3 micron
  However ‘special purpose’ or ‘superfine’ fibres have diameters in the range 0.1 – 3 micron

## Slide 31: Toxicity of fibres
Fibre toxicity determined by dose, dimension and durability
Diameter of the fibre is critical in determining where the fibre deposits in the lung
  Fibres of diameter 3 micron or greater do not reach the deep lung
  Most machine made mineral fibre diameters are greater than 3 micron and do not split along their length into finer fibres
  Most asbestos fibres have diameters much less than 3 micron and can split along their length into finer fibres
Fibre durability (or bio-persistence) determines how long it will remain in the lung
  Half life of MMMF in the lungs varies from days to months
  Half life of chrysotile in the lungs is months to a few years
  Half life of amphibole fibres in the lungs is several decades

## Slide 32: Other common man made fibres
Carbon fibres
  Typically 5 – 15 micron diameter fibres
  Flexible, light, strong, corrosion resistant
  High abrasion and wear resistance
  Poor insulators
  Used in advanced composite materials to improve strength, durability or electrical conductivity
Aramid fibres (e.g. Kevlar and Twaron)
  Typically 12 – 15 micron diameter fibres, however small (< 1 micron) diameter fibrils also present
  Very strong, flexible, resistant to heat, chemicals and abrasion
  Used in advanced composite materials to improve strength and durability

## Slide 33: Other common man made fibres
Polyolefin fibres
  Long chain polymers
  Polyethylene and polypropylene widely produced and used
  Typically greater than 10 micron diameter fibres
  Low tensile strength and melt at low temperatures
  Typically used in textile applications such as carpet backings, textiles and ropes