## Slide 1: M504 – Bulk Analysis

## Slide 2: Bulk Analysis - Introduction
This session will not make you competent analysts!
Aim is to make you aware of how samples are analysed and the limitations of the method
Each asbestos type has slightly different chemical composition and crystal structure
  These differences are used to distinguish between the asbestos types (and between asbestos and other fibres)

## Slide 3: Bulk Analysis - Introduction
Multi stage process starting with initial examination by eye, then under low power microscopy, leading to a tentative identification
Some fibres that have been tentatively identified are examined using polarised light microscopy at high magnification to confirm fibre type
Note: Polarised light microscopy is the most widely used method but other methods are available.

## Slide 4: Health and Safety Precautions
Asbestos fibres need to be released from the sample matrix, so appropriate precautions must be in place
All initial examination and sample preparation should be undertaken inside a safety cabinet
  Minimum face velocity of 0.5m/s.
  Fitted with a high efficiency “HEPA” filter.
  Visual indicator showing correct functioning
  Checked every day
  Tested every 6 months
Risk assessments and precautions for working with acids, solvents and refractive index liquids

## Slide 5: Typical safety cabinet

## Slide 6: Initial Examination
Entire sample examined by eye
  Initial assessment of possible type of asbestos product
  Visible fibres present or not?
  If sample non-homogenous each part examined
Examination of sample using low power microscope
  Visible fibres present or not?
  Initial assessment of type(s) of fibre present
  Very fine fibres may still not be seen at this stage
  Appearance, colour and texture of any fibres noted and recorded

## Slide 7: Sample Preparation
Purpose of sample preparation
  Ensure fibres released from sample matrix
  Remove fine particles adhering to fibres
  Obtain dry fibres (essential for dispersion staining)
Sample preparation techniques include
  Physical extraction – tweezers, scraping of surface
  Acid digestion
  Solvent extraction
  Combustion (below 400oC)
  Wet grinding

## Slide 8: Stereo microscopy
Examination of sample inside safety cabinet
  Colour (blue, white etc)
  Elasticity (does the fibre return to its original shape when distorting force removed)
  Tenacity (resistance to breaking)
  Morphology (its form, structure)
  How fine are the fibres?
  Are the fibres in bundles?

## Slide 9: Stereo microscope examination

## Slide 10: Stereo microscope examination

## Slide 11: Stereo microscope examination

## Slide 12: Transferring fibres onto slide
Tentative identification of fibres is used to select the most appropriate refractive index liquid for subsequent analysis
  Fibres that are dry, relatively free from other adhering particulate matter chosen
  Placed into a drop of refractive index liquid on microscope slide
  Glass cover slip placed on top of liquid drop

## Slide 14: Refractive index liquids

## Slide 15: Polarised Light Microscopy
Light is a type of energy that travels in the form of a wave
  Ordinary (un-polarised) light contains light vibrating in all directions
  Polarised light has a single vibration direction
  Ordinary light can be polarised with a polarising filter
Some materials e.g. glass, some plastics are isotropic – they only have one refractive index
Many materials e.g. asbestos fibres, many crystalline materials are anisotropic – they have more than one refractive index
Polarised light is used to study anisotropic crystals

## Slide 16: Colour and pleochroism
Pleochroism – coloured anisotropic substances show different colours at different orientations relative to polarised light
Crocidolite fibres showing pleochroism

## Slide 17: Birefringence
Anisotropic materials have different refractive indices
The numerical difference between the different refractive indices is the birefringence i.e.
  Large difference in refractive indices – high birefringence
  Small difference in refractive indices – low birefringence
Anisotropic materials show maximum interference colours and / or brightness against a dark background when aligned at about 45o to the vibration plane of the polarised light

## Slide 18: Birefringence

## Slide 19: Birefringence

## Slide 20: Birefringence
Crystalline materials with more than one refractive index (anisotropic) show birefringence under crossed polars.
Isotropic materials (for example, glass fibre) have only one refractive index and do not polarise the light transmitted through them
  They show no birefringence and are distinguished easily from asbestos under cross polars - they are barely visible but will be seen easily with slightly uncrossed polars

## Slide 21: Angle of extinction
As the microscope stage rotates, an asbestos fibre viewed between crossed polars will disappear from view or “extinguish” at four positions each 90o apart. Between each extinction interference colours should be visible.
Chrysotile, amosite, crocidolite and anthophyllite extinguish when the fibre is parallel to the vibration orientation of the polariser or analyser.
  Actinolite and tremolite asbestos exhibit parallel or very nearly parallel (less than 5o from parallel) extinction.

## Slide 22: Sign of elongation
The colour changes indicate whether the high refractive index vibration plane of the fibre is parallel to the long or short axis of the fibre (i.e. length fast or length slow)
Crocidolite is the only asbestos type which usually shows a negative sign of elongation (length fast)
  Note: This can reverse if the fibre has been subjected to high temperatures

## Slide 23: Sign of elongation
Chrysotile fibres

## Slide 24: Dispersion staining
Dispersion staining colours will be observed when the fibre is immersed in a liquid with a refractive index close to that of the fibre in question
Different colours will be produced when the fibres are oriented parallel or perpendicular to the polariser
The presence of the correct dispersion staining colours is the final piece of evidence to confirm the identity of the asbestos fibres (which up to this point has only been a tentative identification)

## Slide 25: Dispersion staining
To produce dipersion staining colours the fibre must be immersed in a liquid with a refractive index close to that of the fibre in question
There are different refractive index liquids commercially available
The following refractive index liquids are used for asbestos identification
  1.700 Crocidolite
  1.670 Amosite
  1.640 Actinolite
  1.605 Anthophyllite and Tremolite
  1.550 Chrysotile

## Slide 26: Dispersion staining
Chrysotile fibres in refractive index liquid 1.55

## Slide 27: Analysis of amosite
Analysis of amosite

## Slide 28: Analysis of chrysotile
Analysis of chrysotile

## Slide 29: Quality control
Bulk analysis should only be undertaken by a trained and experienced analyst
Organisation should have a in-house quality assurance programme in place
In addition the organisation should take part in an external proficiency testing scheme e.g. AIMS or BAPAT
In many countries accreditation to ISO17025 is mandatory e.g. UKAS, NATA, AIHA
There are some recommendations on the maximum number of that should be analysed in a day

## Slide 30: Detection limits
In theory the method is capable of detecting as little as 1 part per million asbestos in a sample
  However, it is likely that this level of contamination may often not be detected
It is important that any cross-contamination of samples is avoided
Note: Percentage of asbestos in a sample cannot be determined by the method described earlier

## Slide 31: Detection limits
Most asbestos containing products contain at least 0.1% asbestos
Many authorities define asbestos-containing in terms of licensing or waste regulation requirements
  This is often set at 0.1%
  Materials with less than 0.1% asbestos are not ‘asbestos-free’ but may be at a level where the risk assessment may not raise special concerns

## Slide 32: Interfering products and fibres
The analytical method can differentiate between the 6 asbestos types
It can also differentiate between asbestos and other fibres such as glass fibre, vegetable fibres, refractory ceramic fibres etc
  However, some fibres show similar characteristics on examination which may lead to problems in analysis – an experienced analyst should be able to distinguish them
  Substances that may interfere include shredded polyethylene, leather swarf fibres, aramid fibres, some natural organic fibres, talc fibres and some mineral fibres